# General

## SECTION INCLUDES

### Formed metal wall panels.

### Accessory components.

## RELATED REQUIREMENTS

### Section 05 12 00 - Structural Steel:  Structural steel building frame

### Section 07 62 00 - Sheet Metal Flashings and Trims

### Section 07 92 00 - Joint Sealants

## REFERENCE STANDARDS

### American Society for Testing and Materials (ASTM):

#### ASTM A653/A653M-23, Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process

#### ASTM A792/A792M-23, Standard Specification for Steel Sheet, 55% Aluminum-Zinc Alloy-Coated by the Hot-Dip Process

#### ASTM A755/A755M-18(2024), Standard Specification for Steel Sheet, Metallic Coated by the Hot-Dip Process and Prepainted by the Coil-Coating Process for Exterior Exposed Building Products

### Canadian Standards Association (CSA):

#### CSA-S136-16, North American Specification for the Design of Cold-Formed Steel Structural Members

### Canadian Sheet Steel Building Institute (CSSBI):

#### CSSBI 20M-17, Standard for Sheet Steel Cladding for Architectural, Industrial and Commercial Building Applications

#### CSSBI S8-18, Quality and Performance Specification for Prefinished Sheet Steel Used for Building Products

## QUALITY ASSURANCE

### Structural design in accordance with CSA-S136.

### Manufacturer Qualifications:  Company specializing in manufacturing the Products specified in this section with minimum 5 years documented experience.

### Installer Qualifications:  Company specializing in performing the work of this section with minimum 5 years documented experience and approved by the manufacturer.

## DELIVERY, STORAGE, AND HANDLING

### Section 01 61 00:  Transport, handle, store, and protect products.

### Protect panels from weathering by removing or venting sheet plastic shipping wrap.

### Store prefinished materials off ground, protected from weather, to prevent twisting, bending, and abrasion, and to provide passive ventilation.  Slope metal sheets to ensure drainage.

### Prevent contact with other materials which will cause discolouration, staining or corrosion.

## WARRANTY

### Section 01 78 00:  Warranties

### Provide manufacturer’s 2-year warranty against manufacturer’s defects and deficiencies from date of Substantial Performance of the Work.

### Provide manufacturers panel finish warranty including degradation of paint finish under normal atmospheric conditions including colour fading caused by exposure to weather.

#### 40-year film integrity and 30-year chalk and colour change in accordance with CSSBI S8-18

# Products

## MANUFACTURERS

#### Westman Steel Industries.

#### Other acceptable manufacturers offering functionally and aesthetically equivalent products.

#### Substitutions: Refer to Section 01 62 00.

## DESCRIPTION

### System Description:

#### Wall System:  Preformed and prefinished single skin metal siding panels with vertical profile.

## STEEL SHEET MATERIALS

### Aluminum-Zinc Alloy-Coated (Galvalume) Steel Sheet:  ASTM A792/A792M, commercial steel (CS), minimum Grade 230, AZM150 coating designation.

## ACCESSORIES

### Flashing and Trim:  As specified in Section 07 62 00, of same material, colour and gloss as cladding in exposed locations.

### Closures:  Manufacturer's standard metal closures and trims, to suit cladding profile.

### Sealants:  As specified in Section 07 92 00, and as follows:

#### Concealed Sealant:  Tape or compound, non-skinning, non-drying, butyl rubber.

#### Exposed Sealant: ASTM C834, acrylic co-polymer, single component, colour matching cladding.

### Fasteners:  Suitable for design loads and application.

### Site Touch-up Paint:  Air-dry paint finish specifically designed for repainting of sheet steel.

### Bituminous Paint:  Asphaltic base.

### Expansion Joints:  Same material, thickness and finish as exterior sheets type, of profile to suit system.

### Anchors:  Galvanized steel.

## COMPONENTS

### Cladding Panels: Prefinished Galvalume steel, lapped edges with exposed fasteners, panel joints.

#### Panel Profile: AWR, 914mm wide.

#### Thickness: 0.76mm core steel thickness.

#### Coating: Sheet steel coil coated to ASTM A755 Silicon Modified Polyester coating.

#### Colour: QC#8062 Charcoal.

# Execution

## EXAMINATION

### Verify existing conditions before starting work.

### Verify dimensions, tolerances, and method of attachment with other work.

### Verify site measurements are as indicated on Drawings.

### Report unsatisfactory conditions to Consultant in writing; Do not start work of this section until unsatisfactory conditions are rectified.

## INSTALLATION

### Install components to CSSBI 20M and manufacturer's written instructions.

### Flashing:  Install starter flashing, drip and other flashing, corners, edgings, and window and door flashings as shown on Drawings.

### Exterior Cladding:

#### Install wall cladding to manufacturer's standard installation procedures, providing proper laps true to line, and tight fitting to ensure a weather-tight face.

#### Install finishing flashing, cap flashing, trims and closures.

#### Attach components in manner not restricting thermal movement.

### Sealants:  Install sealants at junctions with adjoining work as shown on Drawings, in accordance with Section 07 92 00.

## CLEANING

### Section 01 74 00:  Final Cleaning, and as follows:

#### Remove site cuttings from finished surfaces, edges, trims and flashings.

#### Clear weep hole obstructions.

#### Remove temporary protective coverings and strippable films, if any, as soon as each panel is installed.

#### Clean and wash prefinished surfaces with mild soap and water, rinse with clean water.

### Repair and touch up minor surface damage.

### Replace damaged panels and components that cannot be repaired.

END OF SECTION